The glass continues the pharmaceutical 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

9307 high viscosity glass continues the pharmaceutical D82 13000 glass , metal in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 10 sec 

9309 high viscosity glass continues the pharmaceutical D84 18000 glass , metal 

9310 medium-sized viscosity glass continues pharmaceutical D75 3400 crystals , glass , metal 

Low viscosity 9311 , large coating D75 90 glass of area , metal 

9312 glass continues D75 6000 crystal , glass , metal of pharmaceutical (3493 ) 

9313 glass continues the D78 13000 glass , metal of pharmaceutical (349 ) 

9314 glass continues D78 8000 crystal , metal of pharmaceutical (349 ) 

9316 glass continues the D70 20000 glass , metal of pharmaceutical (352 ) 

9317 glass continues the D75 540 glass , metal of pharmaceutical (3492 ) 

9350 glass continues the pharmaceutical D78 1000 glass , metal 

9351 glass continues the pharmaceutical D76 2200 glass , metal 

9353 glass continues the pharmaceutical D76 100 glass , metal 

9358 glass is mended and sewn, the glue line hide 20 glass sunlight of D80 and is tanned by the sun 1hr 

The plastics continue the pharmaceutical 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

9305 plastics , glass , metal continue pharmaceutical D55 100 PC , ABS , Acrylate, Glass is in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 10 sec 

9320 is suffused with continuing pharmaceutical D70 3750 PC with the type plastics, Acrylate 

9321 is suffused with continuing pharmaceutical D65 1000 PC with the type plastics, ABS,Acrylate 

9322 plastics continue D40 400 PC of pharmaceutical (3311 ) , ABS , PVC, PS 

9323 plastics continue D55 4000 PC of pharmaceutical (3523 ) , ABS , PVC, PS 

9326 plastics are continued, the surface scribble and put D50 3300 PC , ABS , Acrylate, PS 

9329 plastics are continued, the surface scribble and put D70 7000 PC, ABS,Acrylate 

9333 plastic surface changes the quality pharmaceutical ------
3500 Acrylate,ABS 

9342 plastics continue pharmaceutical D55 1000 PC , ABS , Acrylate, PS 

9343 plastics continue pharmaceutical D63 13000 PC , ABS , Acrylate, PS 

9344 plastics continue pharmaceutical D40 150 PC , ABS , Acrylate, PS 

9345 plastics continue pharmaceutical D64 9000 PC , ABS , Acrylate, PS 

9346 plastics continue pharmaceutical D50 100 PC , ABS , Acrylate, PS 

It is low to shrink the optics counterpoint to use 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

9032 can only harden , low to shrink, carry projection type optics engine continue D80 20000 iron , aluminium , 10 sec under the purple other light source 365nm intensity of illumination 140mW/cm2 of glass 

Section is caulked waterproofly, resists low temperature D65 20000 irons , aluminium , glass outside 9211 satellite antennas of LNB 

9343 hard disk screw regular glue D68 3000 irons , aluminium , PCBs 

It is hardenned that 9401 is only hot and double , it is low to shrink, connector regular 15000 irons of D85 , aluminium , copper , nickel , PET of optic fibre are in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 30 sec 

It is hardenned that 9404 is only hot and double , it is low to shrink, connector regular 15000 irons of D87 , aluminium , copper , nickel , PET of optic fibre 

The surface scribbles and puts using 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

The hard quality surface of EX-A276 scribbles and puts, resists wear-resisting D72 1500 PC alive, silicon rubber in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 10 sec 

The soft surface of EX-A277 scribbles and puts, resists wear-resisting A30 1500 PC alive, silicon rubber 

The hard quality surface of EX-A297 applies and puts, CD Laquer D84 30 PC 

The soft surface of EX-A344 scribbles and puts, resists wear-resisting A37 2500 PC alive, silicon rubber 

The hard quality surface of EX-A347 scribbles and puts, resists wear-resisting D70 1300 PC alive, silicon rubber 

Electronic part encapsulation using 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

9402 PCB part's dampproof insulating coating 
------------------PCB is in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 10 sec 

Model 9337 SMD LED encapsulation D82 ----------
BT board 



Enclose , PET in 9339 loudspeakers and glue A20 50 sound 

Encapsulation D52 18000 pottery of EX-648 SMD , copper 

EX-A262 is able to bear the encapsulation D76 400 pottery of warm SMD , copper 

Soft board of encapsulation D38 6700 printed circuit of EX-822 enameled wire 

Soft board of encapsulation D70 20000 printed circuit of EX-A400 enameled wire 

Sense pressing type ( PSA) 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

9341 glass / the glass laminates, PDA panel --------
1400 Glass is in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 10 sec 

EX-A236 glass / PET continues, touches and accuses of the screen ---------
1600 Glass,PET 

EX-A299 glass / PET continues, touches and accuses of the screen --------
2700 Glass,PET 

EX-A333 PET continuing 
--------2000 PET 

Only harden the epoxy resin (UV-EPOXY ) 

Serial number of the products 
Characteristic / the viscosity of hardness of application continues sills and hardens the speed 

EX-553 is able to bear solvent , low shrinking , high Tg D82 3000 glass in the purple other light source 365nm intensity of illumination 140mW/cm2 lower 10 sec 

EX-554 is able to bear solvent , low shrinking , high Tg D83 25000 glass 

EX-724 is able to bear shaves , low wears and tear , able to bear solvent D63 30000 PCsinging 

EX-915 is able to bear the solvent type , wine bottle ornaments and include and soak D70 5000 glass 

The silicon rubber of EX-A91 / PET continues, note type keyboard D30 5000 silicon rubbers of computer , PET 

